## Slide 1
  Complex material datasets challenge machine learning due to sparse features.
  Composition crucial: composition proportions overlooked.
  Compositional features present: Atomic info missing.
  XenonPy: 58 elemental points,406 extended dimensions.
  Grayscale images for CNN extraction.
Densification and Visualization of Material Composition Characteristics for Enhanced Materials Property Prediction
Introduction
Densification and Prediction: Atomic features for 2D grayscale images; MCVN predicts steel properties, classifies amorphous alloys. [See Figure A]
  Expert-based visualization: Enhances compositional features in material ML tasks.
  Multimodal deep-network model: Integrates visualization images & raw features, improves accuracy. [See Figure B]
This approach enhances model performances on small sparse matrix samples by expanding material composition data, offering a universal paradigm for predicting material properties.
Feature Enhancement: Densifies sparse composition, boosts generalization.
Modal Translation: XenonPy, element-level features, multimodal grayscale dataset.
Multimodal Learning: MCVN enhances material property predictions.
7th Forum of Materials Genome Engineering
Modal Translation
Results
Conclusion
Figure A. Better utilization of composition for material property prediction using the MCVN.
Figure B. Material composition visualization network architecture.
Regression Task
Yeyong Yu a, Xing Wu a, Quan Qian a, b, *
a. School of Computer Engineering and Science, Shanghai University
b. Materials Genome Institute, Shanghai University, Shanghai
Chinese Academy of Engineering
Materials Genome Engineering
Classification Task
7th Forum of Materials Genome Engineering
Methods
Self-attention Mechanism: Reduces external info reliance, captures internal relevance effectively.
Process Flow: Feature Enhancement with Xenonpy.
Arrangement: Template of compositional features.
Grayscale Image: Element-level description of features
NIMS's steel dataset: 4% 𝑅² improvement (0.92 avg. 𝑅²)
SRIM's steel dataset: 𝑅² = 0.835 on EL (vs 0.64 avg. 𝑅²).
Unbalanced amorphous alloy dataset: Increased avg. 𝑅𝑒𝑐𝑎𝑙𝑙 (CRA small-class) from 0.58 to 0.78.
Regression Task
Reference
Better utilization of materials’ compositions for predicting their properties: Material composition visualization network[J]. Engineering Applications of Artificial Intelligence
FTAP: Feature transferring autonomous machine learning pipeline[J]. Information Sciences